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Cement Typeof Compressive strengths (N/mm?)

strength coarse Age (days)
class aggregate 3 i 28 9
425 Uncrushed 22 30 42 49

Crushed 27 36 49 56
525 Uncrushed 29 37 48 54

Crushed 34 43 55 61

Throughout s publication concrete strength s expressed i the unts N/’
AN/mem? = 1 M/’ = 1 MPa. (N = newton: Pa = pascal)
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Slump (mm) 0-10 10-30 30-60 60-180
Vebe time (s) >12  6-12 3-6 0-3
Maximum size

ofaggregate  Type of

(mm) aggregate

10 Uncrushed 150 180 205 225
Crushed 180 205 230 250

20 Uncrushed 135 160 180 195
Crushed 170 190 210 225

40 Uncrushed 115 140 160 175

Crushed 155 175 190 205
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